Evaluation Methods and Rules for

WOCA AWARDS

[2025 Edition]

Host: World of Concrete Asia

WOCA AWARDS will conduct on-site performance tests on candidate projects in accordance with international standards. The final scores will be obtained by weighting the evaluation values of each dimension for comparison.

Section 1: Scope and Requirements of Participating Projects

- Floor Types and On-Site Inspection Items Covered by WOCA AWARDS (Mainly Based on European Standards):

- BS EN 8204-2 “Guide to Surfacing Concrete”

Concrete surface floors include:

[A-1] Concrete floors used as the surface layer after direct finishing.

[A-2] Concrete floors with cement-based wear-resistant materials on the surface.

[A-3] Concrete floors with penetrating liquid hardeners applied to the surface.

[A-4] Concrete floors with both cement-based wear-resistant materials and liquid hardeners applied to the surface.

- BS EN 8204-3 “Guide to Polymer-Modified Cement Screeds and Wear-Resistant Surface Layers for Floors”

BS EN 8204-7 “Pumpable Self-Levelling Mortars”

Cement mortar surface floors include:

[B-1] Self-levelling polymer-modified cement mortar floors for the surface layer.

[B-2] Non-self-levelling polymer-modified cement mortar floors.

[B-3] Polyurethane-modified cement mortar floors.

[B-4] Epoxy-modified cement mortar floors.

[B-5] Polymer-modified cement mortar bedding + cement-based terrazzo surface layer.

- BS EN 8204-6 “Guide to Resin Floors”

*For the resin floors participating in the selection, the underlying bedding (concrete floor or cement mortar floor) must be constructed by the same contractor, that is, it must be a so-called "integral floor".

The integral resin floor system includes:

[C-1] Concrete or mortar bedding plus types 1-3 resin surface layers specified in Table 1 of BS EN 8204-6.

[C-2] Concrete or mortar bedding plus types 4-5 resin surface layers specified in Table 1 of BS EN 8204-6.

[C-3] Concrete or mortar bedding plus types 6-8 resin surface layers specified in Table 1 of BS EN 8204-6.

[C-4] Concrete or mortar bedding plus epoxy terrazzo surface layer.

Note: Types 1-3 in Table 1 are thin- or thick-coated surface layers with a thickness of less than 1mm applied by brushing; types 4-5 are multi-layer or self-levelling surface layers; types 6-8 are mortar surface layers.

- On-Site Inspection Items and Floor Types

| On-Site Inspection Items | Floor System Classification |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Concrete Surface Floor |  |  |  | Cement Mortar Surface Floor |  |  |  |  | Integral Resin Surface Floor System |  |  |  |
|  | A-1 | A-2 | A-3 | A-4 | B-1 | B-2 | B-3 | B-4 | B-5 | C-1 | C-2 | C-3 | C-4 |
| Floor Flatness |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Surface Wear Resistance |  |  |  |  |  |  |  |  |  | * | * | * | * |
| Surface Bonding Strength | * | * | * | * |  |  |  |  |  |  |  |  |  |

Conduct inspection

*   Do not conduct inspection

- Requirements for On-Site Inspection

- The construction area of the floor project is larger than 1,000 square meters.

- The floor project is completed before November 30, 2025.

- Since the surface wear resistance inspection and surface bonding strength inspection will cause slight damage to the floor surface, the participating unit or the owner should first sign the "Letter of Notification for WOCA AWARDS" to indicate that they are aware of this situation.

Section 2: Inspection Methods, Standards and Judgment Bases

- On-Site Inspection Methods and Inspection Standards

| Inspection Items | Instrument Name | Evaluation Standard |
| --- | --- | --- |
| Floor Flatness | DIPSTICK 2285 | ASTM E-1155 |
| Surface Wear Resistance | Floor Wear Tester NMY-1 | BS EN 13892-4:2002 |
| Surface Bonding Strength | Adhesion Tester PosiTest AT-A | ASTM D7234 |

- Judgment Standards for Inspection Results

| On-Site Inspection Items | Floor System Classification |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Concrete Surface Floor |  |  |  | Cement Mortar Surface Floor |  |  |  |  | Integral Resin Surface Floor System |  |  |  |  |
|  | A-1 | A-2 | A-3 | A-4 | B-1 | B-2 | B-3 | B-4 | B-5 | C-1 | C-2 | C-3 | C-4 |  |
| Floor Flatness | 50 | 50 | 60 | 60 | 40 | 25 | 25 | 25 | 50 | 60 | 55 | 60 | 55 |  |
| Surface Wear Resistance | 50 | 50 | 40 | 40 | 20 | 50 | 45 | 45 | 20 | - | - | - |  |  |
| Surface Bonding Strength | - | - | - | - | 40 | 25 | 30 | 30 | 30 | 40 | 45 | 40 | 45 |  |

- Single-Item Full-Score Rule (Prior to Weighted Calculation)

- When the following benchmark indicators are simultaneously met, the relevant inspection item will be directly rated as a full-score in that indicator category.

      - Floor Flatness value: FF value ≥ 50 and FL value ≥ 50.

      - Wear resistance inspection: Wear amount ≤ 0.05 mm.

      - Pull-out strength test: Bonding strength ≥ 3MPa.

- Comprehensive Scoring Mechanism

- For indicators that do not meet the full-advantage options, they will be accumulated by multiplying the test value by the corresponding weighting coefficient.

- The total score calculation adopts the principle of "single-item full-score priority": Indicators that meet the full-advantage conditions are included in the total score as full-scores, and the remaining indicators are calculated as weighted scores.

- Award Evaluation Rules

Basic Awards

- Gold Award evaluation: The project with the highest total score among similar floors (in addition to the floor types mentioned in Section 1: three major categories and 13 sub-categories, classification will also be based on different construction techniques).

- Silver Award tie-breaking rule: The second and third highest total scores will jointly receive the Silver Award.

- Special promotion: Projects with all inspection indicators reaching full - scores can directly win the Gold Award.

Special Awards

- Peak Award:

- Special rule: Remove the single-item full-score restrictions for FF and FL values.

- Evaluation standard: The project with the highest flatness score will be awarded (can be obtained simultaneously with other awards).

Section 3: Registration Details

- Registration Time:

From March 1, 2025 to November 30, 2025.

- Registration Channel:

World of Concrete Asia

Contact: Lizzy Liu

Fixed-line: 021-61573939

Tel & Wechat: 13501781633

Email: Lizzy.Liu@informa.com

- Application Materials (Electronic Version) Include:

- Application form

- Completion acceptance certificate (if available)

- "Letter of Notification for WOCA AWARDS" signed by the owner unit (if the owner unit is inconvenient to sign, the construction unit can sign on its behalf to indicate awareness)

- Copy of the business license

- Copy of the construction qualification certificate (if available)

- More than three project photos, including the overall project view, construction site, and completed effect

- Project overview and construction plan description

- Relevant materials of the construction materials used in the project

- Project floor plan

- Application Fee:

If the application materials are complete, before the floor project enters the "on-site inspection" stage, WOCA will charge a registration fee of 2,000 yuan (RMB) for each declared project.

Section 4: Public Announcement of Awards Results

- WOCA will publicly announce the list of award-winning projects and project evaluation reports through its official website, WeChat platform, etc. on February 1, 2026, to accept supervision. The publicity period is 10 days.

- If there are any objections to the publicity results, the objecting party needs to provide corresponding evidence and request a review by the evaluation committee. The evaluation committee is responsible for feedbacking the review results to the objecting party. If necessary, a qualified third-party can be requested for inspection and appraisal.

- After the publicity period with no objections, WOCA will finally review and approve the list of award-winning projects.

- The award-winning results will be announced at the 2026 World of Concrete Asia, and certificates and trophies will be presented to the winning enterprises in April of the same year.

About World of Concrete Asia

WOCA is the Asian version of WORLD OF CONCRETE series under Informa Markets. Centered around the construction of concrete floors, it extends to vertical building development and covers construction raw materials, construction machinery and equipment, additives, floor cleaning equipment, facilities, and small tools. It provides a professional, open, and diversified international communication platform for the floor construction industry in China.

About Informa Markets

As a global leader, Informa Markets offers a range of platforms. Its business includes more than 550 international B2B events and brands, covering multiple fields such as healthcare, pharmaceuticals, infrastructure, construction and real estate, fashion, hotels, food and beverage, and health and nutrition. It provides professional data and promotes innovation and development through face-to-face exhibitions.

Precautions for On-Site Inspection of WOCA Awards Application

Requirements for On-Site Inspected Floors

- The on-site area must meet the minimum inspection requirements

- The floor project is completed before November 30, 2025

- Since the surface wear resistance inspection and surface bonding strength inspection will cause slight damage to the floor surface, the participating unit should first obtain the " Letter of Notification for WOCA AWARDS" document signed by the owner

- For projects that may cause slight damage during on-site inspection, the inspection points can be negotiated with the owner, and inconspicuous areas can be selected

- The applicant is responsible for the subsequent repair work of the slight damage caused to the ground by the inspection work

- The environment for on-site inspection must be available (confirmed through communication between both parties before inspection)